DECKON PREMIUM METAL CEILINGS

CLIP-IN SYSTEM

DATASHEET

Technical Info:

Product                       : aluminium or galvanised steel

Sizes	                       : 600x600mm, 300x600mm, 600x1200mm std

Thickness                    : 0.50 - 0.70 mm

Surface                       : electrostatic powder coated

Perforation                  : none or 1.8-2.5mm hole diameter with 10-50-100mm bordure

Suspension syst           : hot dip galvanised steel, black

Edge detail                  : 20-30mm up-turns, as specified

Fire Resistance            : class A as steel

Color                          : RAL 9016, standard white

Specification:

Standard clip-in system consists of a concealed supporting structure where demountable tiles can be clipped into the triangular omega main runner. The grid system is not visible. All panels are independently demountable thus enabling easy and fast access to the ceiling void.

VISUAL

TECHNICAL DRAWINGS

PERFORATIONS